Influence of coarse additions on the plasticity and toughness of soil mixtures, Part I: Effect of particle size.

last compiled Wed. 2022-05-04, 2:28 PM

# Abstract

Sand-clay mixtures are commonly manufactured for use on baseball and softball infield skin surfaces. Atterberg plasticity tests may be an informative way to characterize infield mixes because the tests directly measure the soil’s response to changing water content.

Infield mixes contain a range of sand particle sizes. Standard protocols for the Atterberg limit tests mandate that sand >425 μm is removed from the test specimen via washing. This directive makes it difficult to compare mixes, because the effect of the fines’ plasticity may be confounded by removing different amounts of sand.

Three experiments were conducted to re-appraise the practice of removing ‘oversize’ particles from Atterberg limit specimens.

Coarse additions corresponding to five individual mesh sizes of sand (2.0-1.0, 1.0-0.5, 0.5-0.25, 0.25-0.15 0.15-0.05 mm) and silt were mixed with a kaolinitic clay at 0, 20, 40, 60, 70, 75, and 80 percent coarse addition. The liquid limit (LL) and plastic limit (PL) were determined for each mix.

At low coarse addition contents, LL and PL showed a linear decrease per unit coarse addition. This suggests the sand or silt is fully suspended in the clay-water matrix and do not participate in the soil’s behavior. The linear relationship deteriorated above 50% coarse addition for LL and above 30% coarse addition for PL. Mixes containing the largest particles adhered more closely to a linear reduction in LL or PL than finer materials. It is postulated that in a drying soil thread, a greater number of particle contacts among finer sand grains encourages the formation of defects and micro-cracks. These cracks then coalesce to induce premature crumbling relative to mixes with coarser sand.

Results from this research suggest particles with sieve diameter 2000-425 μm need not be removed for Atterberg limit tests. These particles influence LL and PL less than finer sands, which are permitted to remain in the sample. These findings can encourage more useful evaluations of infield mixes with intermediate sand content, and to expedite the LL and PL tests for infield mixes.

# Introduction

## Definitions of soil behavior thresholds

The Atterberg limits represent unique soil water contents corresponding to definite changes in mechanical behavior. Test results can be used to predict soil shear strength, compressibility, and permeability ([McBride, 2002](#ref-McBride2002); [Holtz et al., 2010](#ref-Holtz2010)).

Four principal states of soil are widely recognized: solid, semi-solid, plastic, and liquid ([McBride, 2002](#ref-McBride2002)). A soil transitions through these states as its water content increases. The four states are delineated by three boundaries (thresholds), termed the shrinkage limit (SL), plastic limit (PL), and liquid limit (LL) ([McBride, 2002](#ref-McBride2002)).

In addition to the three above, Atterberg ([1911](#ref-Atterberg1911)) originally identified four additional states termed: upper limit of dense liquid, lower limit of dense liquid, sticky limit, and cohesion limit.

Subsequent researchers including Casagrande ([1932](#ref-Casagrande1932)) deemed the upper and lower limits of dense liquid too difficult to define and that the sticky and cohesion limits pertained more to the workability of clay in ceramics than to agriculture or earthworks engineering.

Geotechnical engineers modified and standardized Atterberg’s original methods for the three remaining thresholds (LL, PL, and SL). The LL test is performed with a mechanical device comprising a brass cup agitated by a rotating cam ([Casagrande, 1932](#ref-Casagrande1932)). Terzaghi ([1925](#ref-Terzaghi1925)) introduced the use of a fixed thread diameter (3.2 mm or 1/8 in) for the PL test. The PL test remains otherwise unchanged from that described by Atterberg ([1911](#ref-Atterberg1911)). Both threshold water contents are measured on a gravimetric basis and conventionally expressed as percentages.

## Oversize particle removal in plasticity tests

Atterberg limit tests are performed only on material <425 μm sieve diameter ([ASTM International, 2018](#ref-ASTMD43182018); [AASHTO, 2020](#ref-AASHTO2020a)). Particles >425 μm are termed “oversize” by ASTM D4318 ([ASTM International, 2018](#ref-ASTMD43182018)). If oversize particles cannot be removed by hand, the standard dictates the sample be wet-sieved over a <425 μm sieve.

The authors are not aware of a fundamental rationale for the choice of 425μm as the upper boundary for Atterberg limit tests, although we may conjecture that it was chosen to match the boundary between ‘medium’ and ‘fine’ sand in Casagrande’s later-published Airfield Classification (AC) scheme. The AC became the Unified Soil Classification System (USCS) and the 425 μm boundary is still in use today ([Casagrande, 1947](#ref-Casagrande1947); [ASTM International, 2020](#ref-ASTMD2487-17)). The position of the boundary has never been questioned in primary literature.

Therefore, when oversize particles are removed in order to conduct the test, the obtained LL or PL must be adjusted to estimate the whole-soil LL or PL.

The whole-soil LL is computed as:

where is the gravimetric water content as a decimal and is the mass percent passing a 425 μm sieve (as a decimal). The whole-soil PL may be obtained using the same calculation ([ASTM International, 2020](#ref-ASTMD2487-17)).

Barnes ([2013](#ref-Barnes2013)) questioned the accuracy of this correction and suggested that the LL correction becomes invalid when the mass of non-clay particles exceeds 50%, and that the PL correction is invalid at even lower non-clay content (about 30-40%).

ASTM International ([2015](#ref-ASTMD15572015)) describes an alternative approach to dealing with oversize particles, termed the replacement or substitution method.  
In this method oversize particles are removed and replaced with an equivalent mass of particles finer than the upper boundary. This method is no longer permitted by ASTM International ([2015](#ref-ASTMD15572015)). Barnes ([2013](#ref-Barnes2013)) adapted the substitution method to Atterberg limit tests and compared its results to the correction method (Equation @ref(eq:oversize-correction-formula)) and suggested the substitution method is invalid for substitutions as low as 10%.

Barnes ([2013](#ref-Barnes2013)) also suggested that when ≥30% of a sample is removed via sieving, the accuracy of whole-soil LL and PL results is compromised. This supports the language in International ([2015](#ref-ASTMInternational2015a)) which states that results computed from oversize content ≥30% may be suspect.

The practice of removing oversize particles and then correcting for their absence is performed due to the limited size of the test apparatus and the fixed thread diameter in ASTM International ([2018](#ref-ASTMD43182018)). There is little available research on the quantitative definition of “oversize.”

## Previous research on the effect of coarse fraction particle size on Atterberg limits

Plasticity is understood to be a property of clay materials ([Guggenheim and Martin, 1995](#ref-Guggenheim1995)). While numerous studies have evaluated the influence of clay mineralogy on plasticity ([Seed et al., 1964](#ref-Seed1964a); [Dumbleton, 1966](#ref-Dumbleton1966a); [Schmitz et al., 2004](#ref-Schmitz2004a); [Holtz et al., 2010](#ref-Holtz2010); [Spagnoli et al., 2018](#ref-Spagnoli2018)), less attention has been devoted to the effect of sand-size and silt-size particles on soil plasticity.

Some researchers have measured changes in the Atterberg limits due to the addition of sand-size or silt-size particles to a fine-grained soil.

Multiple experiments have shown that the size of these particles (termed “coarse additions”) has a predictable effect on LL and PL ([Dumbleton and West, 1966](#ref-Dumbleton1966b); [Sivapullaiah and Sridharan, 1985](#ref-Sivapullaiah1985); [Barnes, 2013](#ref-Barnes2013)). Dumbleton and West ([1966](#ref-Dumbleton1966b)) measured LL and PL of mixtures containing varying amounts of coarse additions with either kaolinite or montmorillonite clay. Mixtures were produced using equivalent amounts of the coarse additions (coarse sand, D50 = 350 μm; fine sand D50 = 110 μm; or silt, <75 μm) Sivapullaiah and Sridharan ([1985](#ref-Sivapullaiah1985)) performed a similar set of experiments using three sizes of coarse particles and either kaolinite or montmorillonite. The coarse particle ranges were 150-425 μm, 150 μm – 75 μm, or silty soil (no particle size distribution given). Barnes ([2013](#ref-Barnes2013)) tested mixtures of London clay with silt (63-2 μm) or two grades of sand (425-212 μm or 212-63 μm).

The findings of all three studies were similar. Each study compared the measured LL and PL to the values predicted by the linear law of mixtures, a term defined by Sivapullaiah and Sridharan ([1985](#ref-Sivapullaiah1985)). The the linear law of mixtures (or more simply, linear law) is analagous to the correction performed after removal of naturally-occurring particles >425 μm (Equation @ref(eq:oversize-correction-formula)). The linear law states that the water content of a soil mixture at its LL or PL is inversely proportional to the % coarse addition:

where is the coarse fraction mass as a decimal and is the water content of the fines as a decimal.

In all three studies, mixtures containing smaller coarse particles had elevated LL and PL compared with their predicted values. However, mixtures containing the larger coarse particles adhered closely to the linear law. In other words, the disparity between predicted and measured values narrowed with increasing particle size. Note that all the above studies used sand exclusively < 425 μm.

A single study ([Rehman et al., 2020](#ref-Rehman2020)) tested the LL and PL of natural soils sieved to pass either a 2000 μm or 425 μm sieve. For soils with LL <35, allowing the particles 2000-425 μm to remain in the sample resulted in  
When the LL exceeded 35, the two sieving procedures resulted in greater differences.

Collectively, these studies demonstrate when coarse particles are added to a fine-grained soil, the size of the particles affects the mixture’s LL and PL. Mixes containing finer “coarse additions” deviate from the linear law while mixes containing the coarsest additions adhere to it more closely.

### Relationship of Atterberg limits to toughness of fine-grained soils

Soil toughness is an important consideration during tillage and earthmoving operations because it governs the energy required to deform, fragment, or compact the soil.

Barnes ([2013](#ref-Barnes2013)) defined soil toughness as the work required to deform a fully ductile soil specimen over a defined strain range. This differs from the definition given by Casagrande ([1932](#ref-Casagrande1932)), which was a soil’s shearing resistance (i.e. peak load) at its plastic limit. Barnes ([2013](#ref-Barnes2013)) considered soil toughness to have its maximum value at the plastic limit.

In the Barnes study ([2013](#ref-Barnes2013)), the size and quantity of coarse additions mixed with clay affected the toughness of the mixtures. The mixtures were compared on the basis of their matrix water content, which was defined as the water content per unit mass <2 μm:

At equivalent matrix water content, mixes with the coarser sand additions had lower toughness. Barnes ([2013](#ref-Barnes2013)) attributed this to a greater number of contacts between smaller particles, which are more numerous per unit mass. However, the soils with the coarser sand also had a lower PL compared to the finer mixtures. This means that the mixes with coarser sand could be dried down further before they became brittle, and their toughness at their respective whole-soil PL was higher than that for the mixtures containing the finer sand grade or the silt.

The toughness research by Barnes [-Barnes ([2009](#ref-Barnes2009)); -Barnes ([2013](#ref-Barnes2013));] was performed using a specialized apparatus which is not commercially available. To expand the utility of the soil toughness concept, Moreno-Maroto and Alonso-Azcárate ([2018](#ref-Moreno-Maroto2018)) re-analyzed data from Barnes ([2013](#ref-Barnes2013)) to develop an empirical correlation between Atterberg limits and . Their empirical equation can be solved to predict from PI and LL:

Note that Equation @ref(eq:moreno-marato-toughness-equation) was developed using pure/natural soils as opposed to artificial mixtures.

## Utility of Atterberg limits and toughness estimates for assessing baseball infield soils

A baseball field comprises 3 main surface types: natural or artificial turfgrass, the warning track, and the infield skin. The infield skin is composed of compacted bare soil and is widely considered the most critical portion of the field ([Zwaska, 2007](#ref-Zwaska2007b)). The behavior of an infield soil is markedly affected by its water content ([Association, 2015](#ref-SportsTurfManagersAssociation2015)). Therefore, the Atterberg limits may offer a means to quantitatively assess infield soil performance. Toughness is also an important consideration of the grounds manager. A tough infield soil allows minimal disruption to the surface from loads imposed by athletes and baseballs.

Infield skin soils are often often dry screened to pass a 2000 μm sieve, but they may still contain up to 50% of their total mass between 2000 μm and 425 μm ([Schroder, 2012](#ref-Schroder2012)). Canonical Atterberg limit methods require much of these samples to be removed. While the whole-soil LL and PL could be computed from Equation @ref(eq:oversize-correction-formula), the linear law correction may be unreliable when coarse addition content exceeds ~30-40% ([Seed et al., 1964](#ref-Seed1964a); [Sivapullaiah and Sridharan, 1985](#ref-Sivapullaiah1985); [Barnes, 2013](#ref-Barnes2013)).

If the linear correction is not used, the removal of particles >425 μm may limit comparison of test results. Consider a case in which two soils contain identical total sand content but different types of fines and different sand-size gradations. These soils will likely have different LL and PL values; however, it will be unclear whether the differences are due to the nature of the fines, or simply because more sand 425-2000 μm was removed.

Given the unreliability of the linear correction for oversize content, and given that infield soils contain a wide range of sand contents and sand sizes, using 425 μm as the upper boundary of acceptable particle sizes may not be the ideal procedure for testing the Atterberg limits of infield soils.

## Objectives

The present research was designed to answer three questions:

1. Can the Atterberg limit tests be successfully performed without removing “oversize” particles 2000 μm-425 μm?
2. How do LL and PL of soil mixtures containing oversize particle compare to those for mixtures containing only particles <425 μm?
3. How do LL and PL of mixtures containing variously-sized coarse additions compare to the values predicted by the linear law?
4. How does the particle size of coarse additions affect the calculated toughness of a soil mixture?

# Materials and methods

## Mixture component characterization

Soil mixtures were produced from seven rates of six different-sized coarse additions and a single kaolinitic clay soil. Particle size analyses were performed on each coarse addition and clay soil according to Gee and Or ([2002](#ref-Gee2002)). Standard sedimentation was used with the the pipette method to compute the percent of the sample finer than 20, 5, and 2 μm. Centrifugation with pipette sampling was utilized to quantify the fine clay fraction (<0.2 μm.) ([Gee and Or, 2002](#ref-Gee2002)). Prior to blending with any coarse additions, Atterberg limit tests were also performed on the clay soil component.


## Mixing procedure


Components were air-dried and their water contents were determined gravimetrically. The clay component was pulverized and passed though a 0.25 mm screen. Coarse additions were mixed by hand with the clay component until visually homogenous. The component percentages were adjusted for the trace amounts of particles between 2000-53 μm in the clay soil. Final mixture percentages are expressed on an oven-dry basis (kg coarse addition kg mixture-1).

## Treatments

This experiment evaluated soil mixtures, each containing one of the six coarse additions mixed with the kaolinitic clay. Each of the six coarse additions were combined in varying ratios to yield final mixtures having 0, 20, 40, 60, 70, 75, and 80 % coarse addition, for a total of 42 mixtures. An angular quartz sand was sieved using a continuous-flow screening device in order to generate adequate quantities of material in 5 size fractions (2-1, 1-0.5, 0.5-0.25, 0.25-0.15, and 0.15-0.053 mm). Each fraction was sieved ≥2 additional times to minimize the presence of particles outside the desired range. Silt-size material (<0.053 mm) comprised the sixth coarse fraction and was obtained from a wholesale ceramic supplier as Sil-co-sil 52 crushed silica (U.S. Silica, Katy, TX). To verify the cleanliness of each fraction, the particle size distributions of each coarse addition were determined using traditional particle size analysis ([Gee and Or, 2002](#ref-Gee2002)) and are shown in Figure [**1**](#experiment-1-particle-size-curves).

The five chosen sand-size classes correspond to particle diameters used in the United States Golf Association method for putting green construction ([USGA, 2018](#ref-USGA2018)). This specification is familiar to sports field managers and is often referenced when comparing infield mixes. Table [**Error! Reference source not found.**](#usga-sieve-sizes-table) shows the particle size ranges of each of the 6 coarse fractions. The D50 values in Table [**Error! Reference source not found.**](#usga-sieve-sizes-table) were determined graphically ([USGA, 2018](#ref-USGA2018)) from [**1**](#experiment-1-particle-size-curves).





**Figure** **1**: Particle size distributions of the 6 coarse fractions in Experiment 1. Dashed grey lines indicate for a given size fraction.

## Atterberg limit test protocol

Atterberg limit tests were performed on each of the 42 soil mixtures. LL and PL tests were performed according to a modified version of ASTM D4318 ([ASTM International, 2018](#ref-ASTMD43182018)). The modification eliminated the wet-sieving procedure so particles between 2000 and 425 μm remained in the sample. Note that 100% of the pure mixture components passed a 2000 μm sieve.

For the LL, a minimum of four data points were collected to plot the flow curve. Three PL threads were rolled and their average value was used as the representative value for the sample.

Estimated toughness values were computed from the equation published by Moreno-Maroto and Alonso-Azcárate ([2018](#ref-Moreno-Maroto2018)) (Equation @ref(eq:moreno-marato-toughness)).

## Statistical analyses and computational environment

Differences in LL and PL across treatments were statistically compared using analysis of variance [general linear models. ] The percent coarse addition and the D50 were each considered as continuous predictor variables. A two-way polynomial model with interaction was fitted to these differences. The base-10 logarithm of the D50 was used as a continuous representation of the coarse fraction variable. This permits a single value to more appropriately represent the entire range of particle diameters within a size fraction and affords greater explanatory power than considering size fraction as a categorical variable. The logarithms of particle diameters are commonly analyzed because the particle-size distributions of many naturally occurring soils and sediments are log-normally distributed ([Simonson, 1999](#ref-Simonson1999); [Brady and Weil, 2007](#ref-Brady2007); [Pettijohn et al., 2012](#ref-Pettijohn2012))

Treatments were considered significantly different when the predictor variable regression slope was significantly different from zero (P < 0.05). Main effects and interactions were tested using Type III Sums of Squares. All analyses were performed using the lm() function in R Language for Statistical Computing ([Team, 2022](#ref-RCoreTeam2022)).


The analyses also utilized several packages within the **tidyverse** framework ([Wickham et al., 2019](#ref-Wickham2019a)) and the authors’ **soiltestr** package <https://github.com/evanmascitti/soiltestr>. Plots were generated using the **ggplot2** package ([Wickham, 2016](#ref-Wickham2016)).

GNU Make ([GNU, 2020](#ref-GNU2020a)) was used to facilitate reproducible analyses by maintaining links between raw data, analysis code, and finished output. The Makefile, raw data, and analysis code are included in the supplemental materials.

# Results and discussion


Measured LL and PL values were compared with predicted values computed from the linear law (Equation @ref(eq:linear-law-of-mixtures)).

There was a significant interaction between coarse addition percent and coarse addition size (Table [**Error! Reference source not found.**](#experiment-1-d50-ANOVA)). Figure [**2**](#experiment-1-atterberg-limit-facets) shows the LL and PL as a function of coarse particle mass, with one panel per size fraction. The dashed lines represent the water contents predicted using the linear law. With the exception of those including silt-sized additions, all soils containing ≥70% coarse addition were nonplastic and cannot be plotted in Figure [**2**](#experiment-1-atterberg-limit-facets).



The LL test results adhered closely to the linear law up to 20% coarse addition. Above 20% coarse addition, adherence was closer for soils including particles with greater D50. The LL of mixtures containing the coarsest sand (2.0-1.0 mm) were nearly identical to those predicted by the linear law, all the way up to 75% coarse addition. Conversely, the LL of finer materials were always higher than predicted. Mixtures including silt-sized material deviated from the linear law with just 20% coarse addition, while mixtures containing the finer sands began to depart from the predicted values at about 40%. The effect of particle size was even more pronounced for the plastic limit. Mixtures containing coarse additions >250 μm still adhered closely to the linear law. Those containing coarse additions <250 μm had elevated plastic limits and began to diverge from the linear law at around 20% coarse addition.


The physical meaning of the significant interaction between the percent coarse addition (Table [**Error! Reference source not found.**](#experiment-1-d50-ANOVA)) and log10(D50)is that the disparity between predicted and measured values widened with increasing amounts of coarse additions. This is grahpically depicted by the distance between the solid and dashed lines in Figure [**2**](#experiment-1-atterberg-limit-facets). However, the plasticity index (PI) was not greatly affected because the LL and PL increased by equivalent amounts.



**Figure** **2**: Liquid and plastic limits as a function of coarse addition content and size. Dashed lines denote water contents predicted by the linear law of mixtures.

Each panel represents the Atterberg limits as a function of the coarse addition D50, with a separate plot for each % coarse addition. This figure more dramatically demonstrates that for mixtures having equivalent coarse addition content, mixtures including larger coarse additions have less influence on LL and PL than finer particles. When only 20% coarse addition is included (second panel from left), the slopes of the lines are shallow because all mixtures performed similarly. The lines steepen with further additions, demonstrating a larger difference in LL or PL between mixes having different sized coarse additions.

Estimated toughness was also compared across mixtures. Barnes ([2013](#ref-Barnes2013)) defined soil toughness as the total work required to deform a specimen to failure at its plastic limit. Estimated toughness values were computed from Equation @ref(eq:moreno-marato-toughness-equation) for all mixtures in Experiment 1 and are plotted against coarse addition content in Figure [**3**](#experiment-1-estimated-toughness). The estimates are of interest because they represent the influence of coarse addition particle size on the toughness of a soil mixture, even though the calculation produced some negative values (a physical impossibility).



**Figure** **3**: Estimated toughness was markedly reduced by finer sands and silt. The toughness of mixtures containing coarser sands more closely resembled that of the pure clay.

All mixtures produced lower than the kaolinitic clay alone. When the percentage of coarse addition was low (≤40%), estimated was similar across mixtures having different-sized coarse additions. At ≥60% coarse addition their estimated were markedly different. A lone exception was the silt-sized material, which had lower than mixtures with corresponding percentage of sand-size additions, even at just 20% silt. Adding 75% coarse additions in the 2000-1000 μm fraction reduced from 32 kJ m-3 to [dynamic reference], while 75% 250-150 μm reduced to zero.

Collectively, these estimates suggest that the toughness of two soil mixtures can differ even when the coarse addition content and PI values are similar. It follows that the toughness of a soil mixture may be controlled by adjusting the size of coarse additions. In this experiment, mixtures containing coarse sands could be dried to a lower water content before reaching the plastic limit. This allows the clay-water matrix to stiffen, yielding a higher toughness at the PL, while mixtures containing the finer sand or silt are more brittle and have lower toughness at their respective plastic limits. If higher toughness is a desired property of a mixture, it should be produced using a the coarsest sand available.

Two potential explanations for the observed phenomena have been described in the literature. Barnes ([2013](#ref-Barnes2013)) suggested that toughness of soil mixtures could be explained by the number of contacts between coarse particles interacting within the clay-water matrix. The coarsest sand used in Experiment 1 had a D50 of 1.4 mm. Assuming a specific gravity of 2.65, 1 gram of these particles comprises 260 individual grains. In contrast, the finest sand had a D50 of 0.09 mm, representing 9.9^{5} particles per gram - a factor of ~3,800. It is likely that far more particle-to-particle contacts occur in mixes containing fine sands and silt.  
As the soil dries, the probability of these fine particles becoming lodged in an unstable configuration would be greater. More water is then required to separate the particles and allow them to slide past one another without crumbling (PL test) or slumping (LL test). This extra water results in higher water contents at both behavioral thresholds.


Dumbleton and West ([1966](#ref-Dumbleton1966b)) proposed that higher LL and PL for mixes including smaller coarse additions are due to their higher specific surface area (SSA). Specific surface area can be calculated for spherical particles as:

where is the particle radius and is the particle density of the soil solids.

In the present study, SSA for each coarse addition was computed by using 2.65 Mg m3 for and taking the representative particle diameter as the D50 of each material. This computation yields SSA values of 15 m2 g-1 for the coarsest sand and 871 m2 g for the silt. This factor of 58 would seem sufficient to produce the observed disparities in water content among the mixtures. Most of the water associates with the clay phase, but some is clearly associated with the sand or silt.

Figure [**4**](#experiment-1-matrix-water-content-at-LL-and-PL) presents an alternative means to consider the water content at each behavioral threshold. The matrix water content is computed by assuming all water is confined to voids between the particles in the clay matrix, and that none associates with the coarse addition. Note that this definition of differs from that of Barnes ([2013](#ref-Barnes2013)), who assumed that plasticity and toughness are derived only from particles <2μm (Equation @ref(eq:barnes-matrix-water-content)). In the present research, was computed as the mass of water per unit clay soil component :

The horizontal lines in Figure [**4**](#experiment-1-matrix-water-content-at-LL-and-PL) represent the water contents for the pure clay at its LL or PL. These lie at the same position as water contents predicted from the linear law. If the water associated only with the clay, would fall directly on these horizontal lines. For the three finest size ranges, at the PL actually exceeds the LL of the pure clay. This is observed by the position of the blue data points above the yellow dashed line. Clearly, the sand and silt grains are contributing frictional resistance and consuming water in order to permit the soil thread to maintain its integrity.



**Figure** **4**: Matrix water contents at the LL and PL for Experiment 1.

The relevant finding from consideration of the is that the inclusion of larger coarse additions interfered less with the LL and PL tests than did particles currently allowed by ASTM D4318.

# Conclusions

## 2022-05-02 version

order - general trend (as particle size <, effect on mix performance >) - we think (based on prior research) this is due to # of particles, surface area, or both Coarser sand gives you lower LL and PL and higher toughness; the toughness is more similar to the clay with nothing added  
- effect on toughness; potentially remind reader why we care about toughness - even if PI and % coarse addition are =, T is different - if you get the same result with less work then you should do it - not necessarily saying that it *should* be changed, just that it *could* be

# Conclusions

LL and PL tests may be useful for evaluating baseball field soils because they directly enumerate soil behavior as a function of water content. Toughness is also of interest to baseball field managers because this property reduces surface deformation during play.

This research compared the measured LL, PL, and estimated toughness of soil mixtures comprising a single clay mixed with varying ratios of coarse additions. All particle diameters of the three finest coarse additions fell below the maximum allowable diameter in standard test procedures (<425 μm), while the three other coarse additions included particles which would normally be removed from the sample prior to testing.

This research also showed that two soils containing an identical mass of coarse particles can generate similar PI values but result in different estimated toughness when the particles are of different sizes.

Under the conditions of this study, the LL and PL predicted by the linear law more accurately aligned with measured values as the coarse addition particle diameter increased. The greatest deviations occurred when silt-size particles were added.

These findings imply there is no detriment to allowing particles up to 2000 μm to remain in a sample during LL and PL tests, and that the data obtained in this way are equally or more indicative of bulk soil behavior *in situ*. Allowing these particles to remain also reduces processing time for soils containing particles up to 2 mm diameter. Together, these advantages could further adoption/utility of these tests for evaluating infield soils.

Therefore, the authors suggest that when performing LL and PL tests on infield mixes, ASTM D4318 be modified to allow particles up to 2 mm.

A limitation of the current study is that toughness was calculated and not measured. Ideally, future research would measure toughness directly. Additional work could also evaluate the effect of particle shape and particle-size uniformity of coarse additions >425 μ.

# Acknowldgements

The measured LL and PL and estimated toughness deviated less from a linear interpolation as the particle size of the coarse additions increased. based on the percent coarse addition. deviated to a lesser degree from the values predicted by linear law.

Atterberg limit tests procedures mandate a maximum particle diameter of 425 μm. An upper limit to particle size is required to ensure smooth groove closure in the Casagrande cup and permit the soil to be rolled into a thin thread. However, the authors are not aware of a fundamental rationale for the choice of 425 μm as the upper boundary. The limit of 425 μm poses a number of challenges when performing the Atterberg limit tests on baseball infield soils.

These soils typically comprise >50% total sand, much of which must be removed using the established procedure. Two options are then available to compare test results from different soils: (1) compare the results without adjustment, or (2) compute the whole-soil LL and PL using a linear correction. If no adjustment is performed, the test results cannot be fairly compared because the the total fines content of the soils are no longer proportional to their presence in the bulk soil. If the second approach is chosen, the computed whole-soil LL or PL would be inaccurate for most infield mixes because prior research has suggested that linear corrections to obtain the whole-soil LL and PL are unreliable when coarse addition content exceeds ~30%. Therefore, neither approach is optimal.

An alternative strategy is to test infield mixes without removing any particles >425 μm,. So long as the maximum particle diameter is <3.2 mm, the soil can theoretically be rolled into a qualifying PL thread.

Infield soils are commonly dry screened to <2 mm. The present research was conducted to determine whether an alternative procedure in which the sample was dry-screened to 2 mm could accurately measure LL and PL. The tests were performed successfully, and mixtures containing the oversize particles actually adhered more closely to the linear law than mixtures containing equivalent amounts of allowable particles. Therefore, the authors suggest that when performing LL and PL tests on infield mixes, ASTM D4318 be modified to allow particles up to 2 mm. This should result in more accurate test results.

Finally, this research demonstrated that the toughness of soil mixtures is affected by coarse addition particle size.

The results of this research can aid soil suppliers and grounds managers develop a more mechanistic design framework for baseball infield mixes.

# References

AASHTO. 2020. AASHTO T 89-13, Determining the Liquid Limit of Soils.

Association, S.T.M. 2015. Sports Turf Managers Association - Management of skinned infields. <https://www.stma.org/wp-content/uploads/2017/11/65d68a00-150d-457e-8708-dcb12717eecc.pdf> (accessed 11 October 2021).

ASTM International. 2015. D1557 - 12e1 Standard Test Methods for Laboratory Compaction Characteristics of Soil Using Modified Effort (56,000 ft-lbf/Ft3 (2,700 kN-m/M3))1. ASTM Standard Guide 3: 1–10. doi: [10.1520/D1557-12.1](https://doi.org/10.1520/D1557-12.1).

ASTM International. 2018. D4318-17, Standard Test Methods for Liquid Limit, Plastic Limit, and Plasticity Index of Soils. : 20. doi: [10.1520/D4318-17E01.](https://doi.org/10.1520/D4318-17E01.)

ASTM International. 2020. Standard Practice for Classification of Soils for Engineering Purposes (Unified Soil Classification System) D2487-17. doi: [10.1520/D2487-17E01.2](https://doi.org/10.1520/D2487-17E01.2).

Atterberg, A. 1911. Die Plastizität der Tone. Intern mitt. boden: 4–37.

Barnes, G.E. 2009. An apparatus for the plastic limit and workability of soils. Proceedings of the Institution of Civil Engineers-Geotechnical Engineering 162(3): 175–185. doi: [10.1680/geng.2009.162.3.175](https://doi.org/10.1680/geng.2009.162.3.175).

Barnes, G.E. 2013. The Plastic Limit and Workability of Soils. <https://www.escholar.manchester.ac.uk/api/datastream?publicationPid=uk-ac-man-scw:212752&datastreamId=FULL-TEXT.PDF>.

Brady, N.C., and R.C. Weil. 2007. The Nature and Properties of Soils. Prentice Hall, Upper Saddle River, NJ.

Casagrande, A. 1932. Research on the Atterberg limits of soils. Public Roads 13(8): 121–136.

Casagrande, A. 1947. Classification and identification of soils. Transactions of the American Society of Civil Engineers 113: 901–991.

Dumbleton, M.J. 1966. Some Factors Affecting the Relation Between the Clay Minerals in Soils and Their Plasticity. Clay Minerals 6(3): 179–193. doi: [10.1180/claymin.1966.006.3.05](https://doi.org/10.1180/claymin.1966.006.3.05).

Dumbleton, M.J., and G. West. 1966. The influence of the coarse fraction on the plastic properties of clay soils- RRL Report No. 36. Road Research Laboratory, Crowthorne, Berkshire.

Gee, G.W., and D. Or. 2002. Particle-size analysis. In: Dane, J.H. and Topp, C.G., editors, Methods of Soil Analysis: Part 4 Physical Methods. Soil Science Society of America, Madison, WI. p. 255–293

GNU. 2020. GNU Make. Free Software Foundation.

Guggenheim, S., and R.T. Martin. 1995. Definition of clay and clay mineral: Joint report of the AIPEA nomenclature and CMS nomenclature committees. Clays and Clay Minerals 43(2): 255–256.

Holtz, R.D., W.D. Kovacs, and T.C. Sheahan. 2010. An Introduction to Geotechnical Engineering. Pearson, New York, NY.

International, A. 2015. [Practice for Correction of Unit Weight and Water Content for Soils Containing Oversize Particles](https://doi.org/10.1520/D4718_D4718M-15). ASTM International.

McBride, R.A. 2002. [Atterberg Limits](https://doi.org/10.2136/sssabookser5.4.c17). In: Dane, J.H. and Topp, C.G., editors, Methods of Soil Analysis: Part 4 Physical Methods. Soil Science Society of America, Madison, WI. p. 389–398

Moreno-Maroto, J.M., and J. Alonso-Azcárate. 2018. What is clay? A new definition of “clay” based on plasticity and its impact on the most widespread soil classification systems. Applied Clay Science 161: 57–63. doi: [10.1016/j.clay.2018.04.011](https://doi.org/10.1016/j.clay.2018.04.011).

Pettijohn, P.E. Potter, and R. Siever. 2012. Sand and sandstone. Springer Science & Business Media.

Rehman, H.U., N. Pouladi, M. Pulido-Moncada, and E. Arthur. 2020. Repeatability and agreement between methods for determining the Atterberg limits of fine-grained soils. Soil Science Society of America Journal 84(1): 21–30. doi: [10.1002/saj2.20001](https://doi.org/10.1002/saj2.20001).

Schmitz, R.M., C. Schroeder, and R. Charlier. 2004. Chemo-mechanical interactions in clay: A correlation between clay mineralogy and Atterberg limits. Applied Clay Science 26: 351–358. doi: [10.1016/j.clay.2003.12.015](https://doi.org/10.1016/j.clay.2003.12.015).

Schroder, E. 2012. Setting a realistic standard for infield mixes: Opinions from the experts. SportsTurf: 8–16. <https://sportsturfonline.com/2012/03/14/setting-a-realistic-standard-for-infield-mixes-opinions-from-the-experts/4637/>.

Seed, H.B., R.J. Woodward, and R. Lundgren. 1964. Clay mineralogical aspects of the Atterberg limits. Journal of the Soil Mechanics and Foundations Division: Proceedings of the American Society of Civil Engineers 90(4): 107–131.

Simonson, R.W. 1999. Sources of Particle-Size Limits for Soil Separates. Soil Horizons 40(2): 50. doi: [10.2136/sh1999.2.0050](https://doi.org/10.2136/sh1999.2.0050).

Sivapullaiah, P.V., and A. Sridharan. 1985. Liquid Limit of Soil Mixtures. Geotechnical Testing Journal 8(3): 111–116. doi: [10.1520/gtj10521j](https://doi.org/10.1520/gtj10521j).

Spagnoli, G., A. Sridharan, P. Oreste, D. Bellato, and L. Di Matteo. 2018. Statistical variability of the correlation plasticity index versus liquid limit for smectite and kaolinite. Applied Clay Science 156: 152–159. doi: [10.1016/j.clay.2018.02.001](https://doi.org/10.1016/j.clay.2018.02.001).

Team, R.C. 2022. [R: A language and environment for statistical computing. R Foundation for Statistical Computing](https://www.R-project.org/). Vienna, Austria.

Terzaghi, K. 1925. Principles of Soil Mechanics: II- Compressive Strength of Clay. Eng. News Record 95(19): 796–800.

USGA. 2018. Unites States Golf Association recommendations for a method of putting green construction.

Wickham, H. 2016. Ggplot2: Elegant Graphics for Data Analysis. Springer-Verlag, New York, NY.

Wickham, H., M. Averick, J. Bryan, W. Chang, L. McGowan, et al. 2019. Welcome to the Tidyverse. JOSS 4(43): 1686. doi: [10.21105/joss.01686](https://doi.org/10.21105/joss.01686).

Zwaska, P. 2007. Infield Soils and Topdressings - Part 2. Sports Field Managers Association of New Jersey: 4–7.